## Slide 1: Welding Defects

## Slide 2: Introduction
Welding is the process of joining metals through fusion and re- solidification
Though undesirable, it is likely to produce some defects.
The level of defects tolerable depends on end use and consequence of failure
Aim is to suitable practices
minimise it by adopting parameters
and sound

## Slide 3: Classification of Welding Defects
1/9/2020
IIW classifies all defects into 6 groups according to their appearance
  Crack- includes all types of cracks such as crater cracks, hot cracks, cold cracks, etc
  Cavity- includes blow holes, porosities, shrinkage, pipes, etc
  Incomplete fusion & penetration- includes lack of fusion, lack of penetration, etc
  Solid inclusion- includes slag, metal oxides, tungsten, wagon track, etc

## Slide 4: Classification of Welding Defects
1/9/2020
Imperfect shape -under cut, under fill, over lap, excessive penetration, improper bead shape, etc
Miscellaneous defects – includes arc strike, excessive spatter, rough surface, uneven ripples, etc
All these defects can be
  Open to surface
  Hidden (Sub-surface or Internal)

## Slide 5: Cracks
A hair line
separation in the Weld
metal/ Parent metal /HAZ
Most dreaded
of all the weld
discontinuities
Occurs in the weldment when localized stresses exceed the UTS of base metal
The reason can be varied, mainly
  Martensite formation due to rapid cooling
  H2 induced stress etc.
  Improper welding practices.

## Slide 6: Welding cracks
Weldability related crack may be
  Hot Cracks - during welding or early solidification, normally in WM
  Cold cracks/Solidification crack – during contraction of the body, mostly in P/M
  Delayed crack/HIC(Hydrogen Induced Cracking) – Much after welding, normally in service, both P/M & W/M
Improper selection of welding process, parameters, welder’s skill affects
7

## Slide 7: Hot Crack Mechanism
Occurs in the plastic stage
Also known as solidification cracking
Can occur with all steels with high S & P
Gross mismatch of MP between Fe & FeS
Other causes too high current, poor joint design, speed too fast and long arcs.
Use low S+P (0.03%) filler material

## Slide 8: Cold Cracks Mechanism
Later stage of cooling, in HAZ
Occurs with combination of factors present
  Too high Residual stresses
  High restraint
  Formation of martensite as the weld cools
  Low temperature environment
Heat input should be limited,
Proper welding sequence

## Slide 11
11/12/14
HIC (Hydrogen Induced Cracking)Mechanism
Starts with lone hydrogen atom diffusing through weld metal at high temperatures (arc) due to elevated solubility.
Enter in the interstitial space in lattice.
Wander freely even at Room Temp.
Re-combine to molecule on GB of the metal matrix.

## Slide 13: Controlling HIC
11/12/14
Use special low-hydrogen electrodes
Diffuse out hydrogen at elevated temp.
Post-heating within 4 hrs of welding
– Specifically for high-strength steels and low alloy steel such as chrome/molybdenum/ vanadium alloys.
Treating surfaces with Ferrosilicates also helps

## Slide 14: Different types of Cracks

## Slide 15: Cracks: Causes & Remedies
Type of crack | Probable Reason | Remedy
Longitudinal | High ‘S’ in Base Material | High ‘Mn’ in Electrode
 | High CE, Thick plate | Preheat Job, DCEN(Direct Current Electrode Negative), Adjust parameters, Reduce speed
 | Too rigid joint | Modify design
 | HIC | Low H2 electrode, Preheat electrode/flux, thorough cleaning of rust, paint, oil
Transverse | Rapid cooling | Increase weaving,Voltage,Current, Preheat job, Shift to SAW if possible
 | Weld size too small | Modify weld design
Crater crack | Incorrect welding | Follow crater filling technique

## Slide 16: Crater Filling Technique

## Slide 17: Porosities/Blow Holes
Porosity is a group of small voids, where as blow holes are comparatively bigger hole or cavity caused by entrapment of gases (H2, CO, CO2, N2 & O2) within the solidified weld”.
Porosity can occur on or just below the surface of a weld.
Porosity in the weld and HAZ may lead to cracking

## Slide 18: Porosities/Blow Holes
1
6
s
Gas porosity or blow
holes
Cluster
porosity

## Slide 20: POROSITY

## Slide 21: Porosities/BlowHoles
electrodes
Causes :
Work piece or electrode contaminated with:-
  Excessive moisture, rust or scale, oil, grease, etc
Long arc
Fast solidification rate
Prevention:-
Preheat
Maintain proper arc length
Use low hydrogen electrode
Follow procedure for baking & storing
1
9

## Slide 22: Over Laps Overlap occurs when molten metal from the Electrode flows over the parent metal and then cools without fusing with the base material.
1/9/2020
2
Tends to produce mechanical notch.
Promotes Fatigue crack at the sharp point Over laps
where the weld metal and base metal come together at the overlapped surface.
0

## Slide 23: OVERLAP

## Slide 24: Over Laps
2
Cause:-
Current too low
Too large deposition in a single run
Longer arc
Slow arc travel speed.
Prevention:
Proper welding technique
Use proper size of electrode
2

## Slide 25: Under Cut
A groove
formed in parent metal
adjacent to the toe of a weld & left unfilled by the weld metal
Generally located at the junction of weld metal & base metal in the toe or root of the weld
Acts as stress raiser in fatigue loading
Reduces the cross-sectional thickness of BM
1/9/2020
2
3

## Slide 26: UNDERCUT

## Slide 27: Under Cut
Cause:
Excessive welding current
Too large electrode dia
Incorrect electrode angle
Longer arc length
Prevention:
Use prescribed welding current for electrode size.
Adjust electrode angle to fill undercut area.
Correct travel speed, arc length, etc.

## Slide 28: Lack of Penetration
Incomplete penetration of the weld
joint root
metal through the thickness of joint or weld metal not extending to the required depth into the
Cause –
Root gap too small
high welding speed
Low heat input
Too large electrode dia
Prevention:
d
Proper joint preparation
Proper heat input & welding spee
Use suitable size of electrode
1/9/2020
25

## Slide 29: Lack of Fusion
Lack of complete melting/fusion of some portion of the weld metal in a joint
May be at the root, sides or between two runs.
Reduces the strength of welds & makes welded structures unreliable.
Cause:-
Low welding current
Excess welding speed
Unfavourable heat input
Prevention:-
1/9/202–0
Maintain proper current & welding speed26

## Slide 30: Lack of Fusion

## Slide 31: Excessive Penetration Weld metal lying outside the plane joining the toes
Cause:
Too wide a root gap
Too high welding current
Slow travel speeds
Prevention:
Correct the root opening and root face
Reduce the wire-feed speed
1/9/2020
2
9

## Slide 32
INCOMPLETE PENETRATION
&
EXCESSIVE PENETRATION

## Slide 33: Spatter
Small globular metal drops / particles thrown out during welding & stick to the base metal surfaces along its length
Loss of metal as no value addition
Excessive spatters aesthetically unacceptable.
1/9/2020

## Slide 34: Spatter
1/9/2020
Cause:
Higher welding current than recommended
Improper flux ingredients
Damp electrodes
Excessive long arc Prevention:
Correct welding current for type & size electrode
Proper arc length & arc voltage
Spatter cure SC-07(Non-toxic, non- pollutant, water based inorganic anti- spatter flux)
  Easy removal by hair brush or by washing.

## Slide 36: Inclusion
Entrapment of foreign solid matter (Slag, Flux, Oxides, W) within weldment, either between passes or between WM & BM
Inclusions can be continuous or intermittent.
  Impairs the ductility of welds
Non- metallic inclusion:-
  Most dangerous
  May be Sulphide, Oxide,
Silicate or Alumina type
  Acts as stress raiser
1/9/2020

## Slide 37: Inclusion
Causes:
–Inadequate cleaning of weld metal between passes
–Rapid rate of welding
–Too large electrode
–improper current
–Long arcs
Prevention:
Maintain proper current & heat input
Proper cleaning of weld
1/9/2020

## Slide 38: Inclusion

## Slide 39: Tungsten Inclusion
Found in case of TIG welding
  Spalling off of Tungsten from electrode
  Appears white in Radiograph whereas Porosities/ Blow holes/Slag etc. appears black
  2- 3% Thoriated electrode prevents spalling

## Slide 40: Arc Strike
Localised HAZ
striking the electrode or the electrode holder against the work, usually adjacent to the weld, causing an unwanted arc
EXAMPLE OF ARC
STRIKE
1/9/2020

## Slide 41: Shrinkage or Contraction Cavity
A cavity formed by shrinkage of weld metal during its
solidification
– Seldom occurs
Shrinkage cavity
1/9/2020

## Slide 42: UNDERFILL

## Slide 43: EXCESSIVE CONVEXITY

## Slide 44: EXCESSIVE CONCAVITY

## Slide 45: EXCESSIVE WELD REINFORCEMENT

## Slide 46: Defects/Causes/Remedies
ies
Defect/Definition | Causes | Remedies
LACK OF FUSION A discontinuity in a weld between weld metal and parent metal | Dirty surface Improper cleaning Current too low Excess welding speed Unfavorable heat | Clean the edge to be welded. Proper cleaning of each bead. Maintain proper current and weld speed.
LACK OF PENETRATION Weld metal fails to fill up to the root or fails to fuse completely the root face of the parent metal | Inadequate joint preparation. Wrong size of electrode. Low heat input. High welding speed. | Proper joint preparation. Suitable size of electrode. Proper heat input and welding speed.
OVER LAP An imperfection at the toe of the weld caused by overflow of weld metal on the surface of parent metal without | Wrong angle of electrode. Too large deposit in a single run. Faulty electrode | Keep correct angle of electrode. use proper size electrode .

## Slide 47: Defects/Caused/Remedies
Defect/Definition | Causes | Remedies
UNDER CUT A groove in the parent metal along the toe of the weld. | High current Higher dia of electrode Wrong electrode angle | Use proper current and polarity incase of DC. Correct size of electrode. Proper angle of electrode
SLAG INCLUSION Non-metallic substance that enter in the weld metal. | Bad cleaning of weld Faulty electrode. Wrong current Rapid rate of welding. Defective weld design. | Proper current and heat input. Proper design and technique. Proper cleaning of weld.
POROSITIES Entrapment of gases in the weld metal. | Contamination of BM excessive moisture in flux Welding during drizzle Long arc. Excessive current. | Clean joint area. store electrodes properly. Follow manufacturer re- baking procedure. Change welding

## Slide 48: Defects/Causes/Remedies
ies
Defect/Definition | Causes | Remedies
LONGITUDINAL CRACKS | High rigidity of joint. High CE of BM. High ‘S’ content in BM Higher hardenability Hydrogen pick up Thick Job High residual stresses | Job preheating & PWHT Use high ‘Mn’ electrode Increase heat input Minimise joint restraints Use low H2 electrode. Follow WPS and welding sequence
TRANSVERSE CRACKS | Improper electrode Rapid cooling of weld Welds too small for the parts to be joined | Use of proper electrode Reduce cooling rate Use larger weld
POOR APPEARANCE | Amperage too high or low Improper Technique Faulty electrode Irregular travel speed | Use specified current. Provide welding TRAINING
EXCESSIVE SPATTER | Arc Blow High Amperage & voltage Long arc | Use Transformer Proper current & voltage Proper arc length

## Slide 49: General Welding Discontinuities
Cold lap

## Slide 50: General Welding Discontinuities
Cluster porosity

## Slide 51: General Welding Discontinuities
Slag inclusions

## Slide 52: General Welding Discontinuities
Incomplete penetration (IP) or lack of penetration (LOP)

## Slide 53: General Welding Discontinuities
Incomplete fusion

## Slide 54: General Welding Discontinuities
Internal concavity or suck back

## Slide 55: General Welding Discontinuities
Internal or root undercut

## Slide 56: General Welding Discontinuities
External or crown undercut

## Slide 57: General Welding Discontinuities
Offset or mismatch

## Slide 58: General Welding Discontinuities
Inadequate weld reinforcement

## Slide 59: General Welding Discontinuities
Excess weld reinforcement

## Slide 60: General Welding Discontinuities
Cracks

## Slide 61: General Welding Discontinuities
Tungsten inclusions

## Slide 62: General Welding Discontinuities
Oxide inclusions

## Slide 63: General Welding Discontinuities
Burn-Through

## Slide 64: General Welding Discontinuities
Porosity

## Slide 65: EVALUATION OF WELDING DEFECTS

## Slide 66: Defects & Its Evaluation
Performance depends on presence or absence of defects in weld joints
Defects impair the mechanical
properties Definition of welding defects:-
“Defects introduced during welding beyond the acceptance limit that can cause a weld to fail”.
All discontinuities are not defects. Discontinuities are rejectable only if they exceed spec requirements

## Slide 67: Defects & Its Evaluation
Radiographic Standards for evaluation of defects:-
IIW standards
ASTM standards
Acceptance standards vary with service requirements
None of the standards allow cracks!
The Radiograph of the joint is compared against the standard Radiographs

## Slide 68: IIW Standards
Five IIW standards with decreasing severity:
–Black
–Blue
–Green
–Brown
–Red
1/9/2020
6
5

## Slide 69: IIW Standards
Black
  A homogeneous weld or a weld with a few small scattered gas cavities
Blue
  Very slight variation from homogeneity wrt one or more of the following defects:
    Cavity
    Shrinkage cavity
    Slag inclusion
    Undercut

## Slide 70: IIW Standards
Green
  Slight variation from homogeneity in the form of one or more of the following defects:-
    Gas cavity
    Shrinkage cavity
    Slag inclusion
    Undercut
    Incomplete penetration

## Slide 71: IIW Standards
Brown
  Marked deviation from homogeneity wrt one or more of the following defects:-
    Gas cavity
    Shrinkage cavity
    Slag inclusion
    Undercut
    Incomplete penetration
    Lack of fusion

## Slide 72: IIW Standards
Red
  Gross deviation from homogeneity wrt one or more of the following defects:-
    Gas cavity
    Shrinkage cavity
    Slag inclusion
    Undercut
    Incomplete penetration
    Cracks

## Slide 73: ASTM Standards
Specified welding defects levels as per ASTM E- 390 Vol-II
–Defects not allowed:-
Shrinkage /Crack
Lack of Fusion
Burn through
Elongated Porosity
1/9/2020
7
0

## Slide 74: ASTM Standards
Defects allowed:-
  Incomplete Penetration up to level-II
  Slag Inclusion up to Level-III
  Undercut up to level-IV
  Porosity:
    Coarse scattered Porosity up to level-II
    Cluster Porosity up to Level-III
    Fine scattered Porosity up to Level- IV

## Slide 75: Metallurgical problem with SS
Sigma (𝜎) phase formation
  A very hard and brittle intermetallic compound of 30 wt.% ~50 wt.% Cr
  Tetragonal crystal structure
  Precipitates between 600°C and 1000°C
  𝜎phase decreases toughness and elongation
  Promotes hot cracking along the 𝛾/𝜎 interface boundaries due to low elongation
  Formation of depleted Cr region
    Reduced resistance to inter grannular, pitting, and
crevice corrosion

## Slide 76: Metallurgical Problems of SS
Issue of 𝜎phase more severe with high Cr
Not so severe with Ferritic SS used in Rlys.
Remedial actions
  Avoid slow cooling in the temp. range of 1000°C to 600°C
  Solution annealing treatment above 10500C

## Slide 77: Metallurgical Problems of SS
11/24/14
Sensitisation or IGC
  Slow heating/cooling or holding at temp. range of 500-8000C,
  Chromium Carbide precipitates along GB
  Depletion of chromium in neighborhood area.
  Corrosion resistance property of that area destroyed or decayed
  Corrosion at GB in corrosive atmosphere.
  Also known as Weld Decay or Knife edge cracking in reference to welding

## Slide 78: Chromium Depletion in GB

## Slide 79: SENSETIZATION OR IGC
Chromium depletion at the grain boundaries or sensitization

## Slide 80: TIME TEMPERATURE CARBON%
Time-temperature-sensitization curves for Type 304 alloys as a function of carbon
content

## Slide 81: TEMP V/S PRECIPITATION
Temperature Range | Precipitation Reactions
Melting point – 2250 °F (1230 °C) | Niobium (Columbium) carbide dissolves Chromium carbides dissolves
2250 to 1450 °F (1230 °C to 800 °C) | Columbium carbide precipitates Chromium carbides dissolves
1450 to 950 °F (800 °C to 510 °C) | Chromium carbides precipitates
950 to 70 °F ( 510 °C to room temp.) | No reaction

## Slide 82: Intergrannular Cracking

## Slide 83: Metallurgical Problems of SS
Remedies:
  To use extra low carbon steel
  To use stabilized base metal & electrode
    Ti, Nb (Cb) or Ta
  Post Weld Solution treatment.
  For welding thin sheet using ductile Austenetic SS filler metal, preheating & post weld heat treatment is not generally required

## Slide 84: Problems Specific to Ferritic SS
Excessive grain growth above 9500C
  Grain coarsening → loss of UTS& toughness
Remedies
  Restrict heat input,
  Restrict inter pass temperature ≤1500C
    Use Heat chalks to assess
    Resort to stagger welding
    Control weaving

## Slide 85: Problems Specific to Ferritic SS
‘475’ embrittlement
  Slow heating/cooling on the range of 400 – 5400C
  Precipitation of chromium rich α phase
    61-83% Cr, bcc, {100} crystallographic plane.
Remedies
  Post weld heat treatment
    Heating at 7900C i.e. below the grain coarsening temperature → Furnace cooling to 6500C→ Rapid cooling to 4000C
  Matching filler wire or fully austenitic filler wire (25/20 type) may be used.

## Slide 86: Problems Specific to Austenitic SS
Most readily weldable amongst all SS
Generally no pre or post weld heat treatments
However, it suffers from micro- fissuring or Solidification cracking. – Micro crack along the GB
More significant 𝜎phase problem due to
  High Cr
  Presence of Mo, Si, Nb, Ti etc.

## Slide 87: Problems Specific to Austenitic SS
Solidification cracking
  Poor solubility of impurities like P, B, S, Se, Si etc. in austenite
  Segregate along GB during solidification
  GB becomes impure & weaker
  Tendency to develop cracks i.e. Micro- fissures under solidification stress.
Remedy
  Having some ferrite (4-5%) in weld metal
  Higher solubility of impurities in Ferrite

## Slide 88: Schaeffler and Delong Diagrams
Constitution diagrams to predict ferrite levels from the composition
By comparing the effects of austenite and ferrite stabilising elements
Schaeffler Diagram
  Ni (eq) = Ni + 30 x C + 0.5 x Mn
  Cr (eq) = Cr + Mo + 1.5 x Si + 0.5 x Nb
Delong Diagram →Refines Schaffler diagram
  Ni (eq) = Ni + 30 x (C+ N) + 0.5 x Mn

## Slide 89: Schaeffler Diagram
11/24/14

## Slide 90: Special Features of Welding SS
11/24/14
Short arc length
  Specially for rutile coated electrode
    As sealing is not as good as basic coated
ones
Longer arc means
  More Chromium loss
  More nitrogen pick up
    Loss of Corrosion resistance in Ferritic SS
    Tendency towards pure austenitic weld
deposit in Austenitic SS→Microfissuring

## Slide 91: Special Features of Welding SS
Restrict Stringer bead < twice elec.dia.
  Lessheat input rate →fast cooling
    Promotes ferrite formation in the weld metal
Minimum Voltage & Current
  Must not cross as recommended by Mfg.
  Empirical rule: 25 times Elec. Dia.
If crossed
  Red hot Electrode
  Flux peel off → Loss of shielding

## Slide 92
THANK YOU